Physical Operation of Diodes

Band Theory of Solids

Some material from: http://hyperphysics.phy-astr.gsu.edu/hbase/solids/intrin.html

Doped Semiconductors

Diffusion and Drift

| Diffusion D Diffusion constant or Diffusivity |  |
| --- | --- |

Drift

pn Junction Under Open Circuit Conditions

| Majority carriers drift towards opposite region. There they recombine with opposite carriers and disappear. A depletion area is created and bound charge is uncovered. A voltage difference is created and a drift current on the minority carries is created to make net current 0 |  |  |
| --- | --- | --- |

pn Junction Under Open Circuit Conditions

pn Junction Under Reverse-Bias Conditions

pn Junction Under Breakdown Conditions

When is large enough to make  (), as can not change, another mechanism produces .

| Zener The Barrier Voltage is large enough to break the Fermi Level, more carriers, an generated | Avalanche The kinetic energy of the electrons is enough tp break covalent bonds and generate |
| --- | --- |

pn Junction Under Forward-Bias Conditions

pn Junction Under Open Forward-Bias Conditions

| Minority Carrier Distibutions The Minority Carrier distributions will increase Id to the required level and the barrier voltage will be reduced by V At the Junction Similarly: |  |
| --- | --- |