SPEED AND FEED CHART

| HIGH SPEED TOOLS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| MATERIAL |  | CUTTING FLUID |  | SURFACE FEET/MINUTE |  | FEED PER TOOTH |
| ALUMINUM |  | SPIRITS, SOLUABLE OIL |  | 200-300 |  | .001-.008 |
| BRONZE |  | SPIRITS, LARD OIL |  | 50-100 |  | .001-.005 |
| BRASS |  | SPIRITS,LARD,SOL OIL |  | 150-300 |  | .001-.005 |
| CAST IRON |  | DRY, AIR JET |  | 100-150 |  | .0005-.004 |
| CAST STEEL |  | SOL. OIL, SULPHURIZED OIL |  | 30-60 |  | .0005-.006 |
| COPPER |  | SOL. OIL, SULPHURIZED OIL |  | 25-Oct |  | .001-.007 |
| MALLEABLE IRON |  | MINERAL OIL DRY |  | 60-100 |  | .0005-.008 |
| MONEL |  | SOL. OIL, LARD OIL |  | 30-50 |  | .0005-.005 |
| NICKEL |  | SULPHURIZED OIL |  | 60-100 |  | .0005-.004 |
| PLASTIC THERMOSET |  | DRY, AIR JET |  | 100-300 |  | .001-.005 |
| PLASTIC THERMAPLASTIC |  | SOL OIL, SOAPY WATER |  | 100-300 |  | .001-.005 |
| RUBBER |  | DRY AIR JET |  | 100-300 |  | .001-.006" |
| SPRING STEEL |  | SOL. OIL, SULPHURIZED OIL |  | 25-Oct |  | .001-.006" |
| STAINLESS (FREE CUTTING) |  | SOL. OIL, SULPHURIZED OIL |  | 60-100 |  | .001-.006 |
| STAINLESS (TOUGH) |  | SOL. OIL, SULPHURIZED OIL |  | 20-27 |  | .0005-.004 |
| STEEL SAE 1000 |  | SOL. OIL, SULPHURIZED OIL |  | 60-100 |  | .001-.005 |
| TOOL STEEL (O1,P20,ETC) |  | SULPHURIZED OIL |  | 215-250 |  | .001-.006 |
| TITANIUM |  | SULPHURIZED OIL |  | 200-250 |  | .0005-.004 |
| ZINC, ALLOY |  | SPIRITS, LARD OIL |  | 200-250 |  | .0005-.006 |
| MILL FORMULAS |  |  |
| SFM= (RPM X DIA ) / 3.82 |  |  |
| RPM= (3.82 X SFM) / DIA. |  |  |
| IPM= FPT X NO. TEETH X RPM |  |
| FPT= IPM / (NO. OF TEET X RPM) |  |
| IPR= IPM / RPM |  |  |
| CUBIC IN. PER MIN = FEED X WIDTH OF CUT X DEPTH OF CUT |

SURFACE FEET BASED ON HIGH SPEED CUTTER.

DOUBLE SURFACE FOOTAGE FOR CARBIDE CUTTERS.

FEEDS ARE ONLY APPROXIMATE AND SHOULD BE ADJUSTED ACCORDING TO CUTTER DIAMETER (LARGER DIA = HIGHER FPT), RIDGIDITY OF SET UP AND SHARPNESS OF TOOL.